| 79 - PINK GLAZE Aspect : shiny Cône : 6 oxidation Composants : En masse : Gerstley Borate 20,68 Néphéline syénite 16,29 EPK (kaolin) 11,34 Carbonate de calcium 19,52 Silice 32,16 Colorant pink (Chrome-étain-calcium) 12,00 Notes : Vary the amount and kind of pink stain to obtain lighter pinks. 12% of darker pink stains will give burgundy colors. Good as a semi?transparent glaze when used without colorant additions, or with other colorants or stains, although it may craze and be opalescent if thick. You must use a Chrome?Tin Pink Stain to get a good pink, Manganese?Alumina stains don't work well with this glaze. Also try direct additions of Chrome oxide and Tin Oxide ? 5% Tin and 0.15% Chrome give a nice burgandy red. Less chrome will give lighter pinks. Possible Health Hazards: Flint: free silica?wear a NIOSH approved dust mask when handling dry material. From Richard Burkett |  | 80 - FLOATING BLUE GLAZE Aspect : semi-opaque, mottled blue Cône : 6 Composants : En masse : Néphéline syénite 47,3 Gerstley Borate 27,0 Silice 20,3 EPK (kaolin) 5,4 Oxyde de fer rouge 2,0 Oxyde de cobalt 1,0 Rutile broyé (Dioxyde de titane : TiO2) 4,0 Colle CMC préparée 1 pte cuillere Notes : from the Chappell book |  | 81 - FLOATING TEA DUST GLAZE Aspect : deep blue-black w/ mottled brown dust Cône : 6 Composants : En masse : Feldspath potassique 23 Néphéline syénite 23 Kaolin 14 Silice 5 Carbonate de calcium 10 Oxyde de fer rouge 5 Dioxyde de manganèse 5 Carbonate de cobalt 5 Rutile broyé (Dioxyde de titane : TiO2) 5 Talc 5 Colle CMC préparée 1 pte cuillere Notes : MIXING: weigh ingredients very carfully, mix in a clean jar. Premix ontents and add distilled water, then add 2 teaspoons CMC, shake vigorously. Sieve two or three times through 60 to 80 mesh screen. Store in airtight container. APPLICATION: stir occasionally during use, as iron tends to settle. Apply to the thickness of a dime by brushing, dipping, or spraying, using clean tools. Allow glaze to dry slightly between coatings and to dry completely before firing. Take care that dust does not settle on the surface during drying. FIRING: Fire to cone 5 oxidation exactly, cool normally. |
| --- | --- | --- | --- | --- |

| 82 - LIGHT YELLOW MATT Aspect : matt Cône : 6 Composants : En masse : Albany slip 25 Gerstley Borate 50 Kaolin 25 Notes : From Harold J. McWhinnie. Glazes of this sort can be strongly marked with rich visuakl textures due to their high flux content. Substitutions for albany slip: (1) barnard clay 25, (2) ball clay 12, iron 12. Also according to a computer analysis of the above glaze the addition of 5 % rutile would improve the durability. |  | 83 - RANDY'S RED Aspect : Cône : 6 Composants : En masse : Gerstley Borate 31,96 Talc 13,86 Kona F4 Feldspar (sodique) 19,80 EPK (kaolin) 4,95 Silice 19,70 RIO (oxyde de fer rouge) 15,00 Notes : From Dianna Rose Downs. |  | 84 - HAPPY'S MIX Aspect : Semi-mat Cône : 6 oxidation or reduction Composants : En masse : Feldspath potassique 30 Spodumène 20 Dolomie 22,4 Cornwall stone (felspath mixte) 25 Carbonate de calcium 3,5 Zircopax (zircon : ZrSiO4) 10 Dioxyde d'étain 8 Bentonite 4 Notes : Semi-mat pale blue (over white clay) additions lite green : 1% black copper brown spotted gold : 10% red clay and 10 % gran. illemanite glue green spotted : 1% cob carb and 1% green chrome and 4% fine manganese diox. |
| --- | --- | --- | --- | --- |

| 85 - GUMP GREEN Aspect : Cône : 5 - 6 oxidation Composants : En masse : Custer feldspar (potassique) 232,4 Carbonate de calcium 91,5 Silice 32,3 Oxyde de zinc 30,4 Kaolin 54,4 Dolomie 6,25 Carbonate de baryum 18,75 Ball Clay 12,5 Oxyde de fer noir 17,7 Carbonate de cobalt 3,5 Notes : From Patrick Veerkamp. apply thinish, best on dark body : dark green matt, black where thin, with kinda yellow overtones. |  | 86 - BEIGE CREPE Aspect : smooth matt Cône : 6 Composants : En masse : Custer feldspar (potassique) 49 Silice 5,3 Carbonate de calcium 18 Oxyde de zinc 8,2 Ball Clay 14,7 Bentonite 4,8 Rutile (Dioxyde titane : TiO2) 6 à 8 Notes : From Janice Lipuma. A medium tan/gold smooth matt. great alone or over others. (the more rutile, the more golden color) |  | 87 - SOFT TURK Aspect : matt Cône : 6 Composants : En masse : Custer feldspar (potassique) 34,9 Carbonate de calcium 12,6 Oxyde de zinc 25,8 Kaolin 4,1 SIlice 22,6 Rutile en grains (dioxyde de titane) 3 Carbonate de cuivre 3 Notes : medium blue green |
| --- | --- | --- | --- | --- |

| 88 - GLOSSY OPAQUE COPPER BLUE Aspect : turquoise Cône : 6 oxydation Composants : En masse : Custer feldspar (potassique) 51 Silice 19 Carbonate de calcium 7 Gerstley Borate 21 Ball Clay 2 Carbonate de cuivre 4 Notes : Can also be made into rutile green by subst. Chrome Ox. 3 and rutile 3for the copper carb. Or, sky blue add cobalt carb 5 and rutile 3(omit copper carb) Very consistent, stores well. I think its from the COMPLETE BOOK OF CLAY AND GLAZES |  | 89 - BARNARD BLACK Aspect : satin matt black Cône : 6 oxydation Composants : En masse : Barnard clay 65 Custer feldspar (potassique) 15 Carbonate de calcium 10 Colemanite 10 Notes : The recipe does not specify which feldspar but Custer seems to work fine. Note: 1. It goes dark brown over a light coloured glaze. 2. Crawls if put on too thickly. 3. Can be used on greenware. 4. Look Ma! No oxides! From Robert Wadey |  | 90 - ROB WADLEY'S BARNARD BLACK Aspect : semi gloss Cône : 6 electric Composants : En masse : Barnard clay 54 Néphéline syénite 29 Gerstley Borate 17 Notes : This was dark brown, well behaved semi-gloss. It's semi-transparent where thin. From Vickie AJohn Sproule |
| --- | --- | --- | --- | --- |

| 91 - OSB Aspect : shino white Cône : 6 Composants : En masse : Kona F4 Feldspar 45 Silice 33 Carbonate de calcium 4 Talc 7 Kaolin 5 Carbonate de soude 5 Dioxyde d'étain 10 Notes : Nice shino white breaking to orange. |  | 92 - R-1000MATT Aspect : Cône : 6 Composants : En masse : Néphéline syénite 38,7 Wollastonite 15,2 Carbonate de baryum 15,2 Gerstley Borate 10,2 EPK (kaolin) 10,2 Silice 10,5 Notes : source for original recipe : Wayne Bate color: black, brown, blue, purple, turquoise, chartreuse, coral, yellow, crimson, and green. surface: matt RM-54 Black - 5% Mason 6600 RM-41 Brown - 10% Mason 6153 RM-53 Blue - 5% Mason 6313 RM-34 Purple - 10% Mason 6385, 5% Wollsatonite RM-37 Turquoise - 10% Mason 6390 RM-47 Chartreuse - 5%, Mason 6236 RM-55 Coral - 15% Mason 6090, 5% Frit 3134, 10% Wollastonite RM-50 Yellow - 5% Mason 6481 RM-44 Crimson - 10% Mason 6006 RM-42 Green - 6% Mason 6219 Mason stains = colorants céramiques |  | 93 - NO NAME GLAZE Aspect : Cône : 6 reduction Composants : En masse : Talc 25 Cryolite 15 Silice 30 EPK (kaolin) 30 Bentonite 2 Notes : submitted by Eliz Drachman |
| --- | --- | --- | --- | --- |

| 94 - ZAKIN'S GK ASH Aspect : Cône : 5 - 6 Composants : En masse : Fritte Ferro 3134 18 Carbonate de magnésium 7 Néphéline syénite 10 Carbonate de strontium 11 Spodumène 15 EPK (kaolin) 10 Carbonate de calcium 13 Opax 12 Bentonite 2 Ash, unwashed fireplace (cendre de bois de foyer de chauffage non lavée) 15 Notes : submitted by Janet Price. Doesn't add to 100 because of the strontium/barium substitution, the bentonite, and the ash. This may be closer to cone 5 than cone 6 but seems to work over a range of a couple cones. This is Zakin's GK base with 15% unwashed, mixed fireplace ashes, with strontium substituted for barium and superpax for opax. By itself over porcelain, the glaze is not particularly interesting. But other glazes on top of it run and drip and blend together nicely. I've found that if I glaze the lower 2/3 or 3/4 of a pot with a well?behaved glossy glaze, brush a coat of this ZGK ash glaze on the top 1/3 or so and then brush or dip some third glaze on top of the ash glaze, I get a nice pattern of runs that don't go off the bottom of the pot onto the kiln shelf (usually). Different glazes give different kinds of runs and bands of different glazes are interesting too. The few times I tried a matte glaze on the bottom, the pots cracked. Could have been coincidence. But I've been sticking with glossy glazes on the bottom since then. |  | 95 - SHIMMER Aspect : matt to glossy Cône : 4 - 8 Composants : En masse : Custer feldspar (potassique) 45 Carbonate de calcium 22 Silice 13 Kaolin 15 Carbonate de lithium 6 Notes : comments: for green, add 6 gr rutile + 2 gr Cobalt Carbonate + 1 gr bentonite , for blue add .5% Cobalt Carbonate AT cone 4-5 these glazes are a wonderful matt; higher they turn 'glossy'. I especially did not like the green at this temperature - too hard and glassy looking. These recipes came from Capilano College in North Vancouver (Canada) where I took a glaze course. submitted by Penny Anagnostopoulos |  | 96 - MATT BLACK Aspect : matt Cône : 6 Composants : En masse : Alnany slip 27,5 Custer feldspar (potassique) 30 Gerstley Borate 6,5 Silice 20 Ball clay 3 Oxyde de zinc 3 Carbonate de calcium 3 Talc 7 Carbonate de cuivre 9 Carbonate de cobalt 6 Notes : These recipes came from Capilano College in North Vancouver (Canada) where I took a glaze course. Another wonderful recipe from there is one for a matt black at cone 6. submitted by Penny Anagnostopoulos |
| --- | --- | --- | --- | --- |

| 97 - SATIN MATT Aspect : Cône : 6 - 4 Composants : En masse : Gerstley Borate 11,18 Dolomie 11,23 Carbonate de calcium 13,70 Oxyde de zinc 0,32 Néphéline syénite 41,37 EPK (kaolin) 5,95 Silice 16,25 Notes : The following is one of my favorite Satin Matts. It fires at cone 06-04 and will accept most colorants. Not every glaze fits every clay body, please test first. submitted by Christine Winokur |  | 98 - MATTE BASE Aspect : matt Cône : 5 - 6 Composants : En masse : Cornwall stone (felds mixte) 74,7 Carbonate de calcium 17,9 Gerstley Borate 5,1 Bentonite 2,4 Notes : A nice, reliable, matte base glaze for Mason Stains. For purple, try adding 5% # 6385 (pansy purple). For green, try adding 5% # 6219 (french green). I like the way it shows speckles when used over Standard Clay # 112. Mason stains = colorants céramiques |  | 99 - VAL Turqouise Aspect : frost Cône : 5 - 9 oxidation or reduction Composants : En masse : Custer feldspar (potassique) 27,6 Gerstley Borate 16,87 Silice 21,32 Carbonate de calcium 8,82 Dolomie 2,9 Carbonate de cuivre 2,34 Bentonite 8 Notes : a pale blue turwuoise with a frost. I recently saw these on test tiles fired at cone 6 oxidation and cone 9 reduction. Both versions of both glazes were very nice. submitted by Michelle Lowe |
| --- | --- | --- | --- | --- |

| 100 - Emerald Green Aspect : frosy Cône : 5 - 9 oxidation or reduction Composants : En masse : Gerstley Borate 49 EPK (kaolin) 19 Silice 32 Carbonate de soude 2 Oxyde de chrome vert 2 Cobalt 1 Notes : Emerald Green ^5-9 oxidation or reduction - a darker green also with a slight dark blue frost. I recently saw these on test tiles fired at cone 6 oxidation and cone 9 reduction. Both versions of both glazes were very nice. submitted by Michelle Lowe |  | 101 - Kickwheel clear Aspect : gloss Cône : 5 - 7 Composants : En masse : Gerstley Borate 50 Silice 32,5 EPK (kaolin) 17,5 Notes : The following is a cone 5-7 clear gloss base, we have made it for over 20 years: It takes most Mason colors and is simple to make. submitted by Christine at Kickwheel Pottery Supply |  | 102 - C. Gareri Base Aspect : Cône : 4 - 8 oxidation Composants : En masse : Néphéline syénite 34,1 EPK (kaolin) 1,8 Gerstley Borate 16,3 Silice 31,8 Carbonate de calcium 3,9 Oxyde de zinc 6,1 Carbonate de baryum 5,9 Bentonite 2 Notes : I have never ommitted Barium in this ^4-^8 oxidation glaze actually i have not used the glaze in years. But it is a great oxidation glaze and I considered using it next year at the school where I teach. However, the barium scared me. IF barium Carb can not be ommited is there a safe substitute - submitted by Charles Gareri |
| --- | --- | --- | --- | --- |

| 103 - Chappel Boron Lithium Aspect : glassy Cône : 6 Composants : En masse : Spodumène 51 Gerstley Borate 26 Silice 23 Carbonate de cuivre 5 Oxyde de fer rouge 0,5 Bentonite 1 Notes : I was looking for something like Warren MacKenzie's Glassy Green that would fire at ^6 instead of ^4. The Boron Lithium in Chappel's glaze book looked close so I added the same oxides as MacKenzie uses in his ^4. MacKenzie doesn't use his ^4 anymore, but found a ^1 glassy green he uses instead. This is also a nice transparent ^6 without colorants. submitted by Lee Love |  | 104 - Mexico Point Green Aspect : matt Cône : 6 Composants : En masse : Kona F4 spar (sodique) 34 Spodumène 14 Kaolin 6 Dolomie 14 Gerstley Borate 12 Zircopax (zircon : ZrSiO4) 20 Carbonate de cuivre 2,5 Bentonite 1 Notes : I'm sending this to the group rather than directly because it's such a nice glaze some others might like to have it too. It's cone 6, from Coopers Electric Kiln Ceramics, Vol.2, p122. Called "Mexico Point Green". It's a lovely soft matte green on the white burning stoneware I use. submitted by Dan Taylor |  | 105 - KLINESVILLE GOLD (Jeff Dietrich) Aspect : golden Cône : 6 electric Composants : En masse : Carbonate de magnésium 4,49 Carbonate de calcium 20,23 Wollastonite 5,62 Néphéline syénite 56,18 Redart clay 13,48 Oxyde de fer rouge 6,74 Zircopax (zircon : ZrSiO4) 12,36 Notes : Golden glaze to round out the palette and add warmth. This applied smoothly - was a smooth satin matt - color similar to old gold. |
| --- | --- | --- | --- | --- |

| 106 - WANAMAKER SATIN GLAZE (Jeff Dietrich) Aspect : satin matt Cône : 6 Composants : En masse : Dolomie 19,28 Spodumène 12,05 Néphéline syénite 54,21 Ball Clay 14,46 Dioxyde de titane (TiO2) 2,41 Oxyde de zinc 4,82 Notes : Finely Textured Satin matt - Do not apply too thick as it will bubble. I substituted Rutile for Titanium Dioxide because I didn't have any and it worked fine. Just don't double dip unless glaze if very thin. I liked how this worked over texture. |  | 107 - Corcoran Black Aspect : Cône : 6 oxidation or reduction Composants : En masse : Carbonate de magnésium 2,6 Custer spar (potassique) 48,3 Carbonate de calcium 17,2 EPK (kaolin) 4,3 Silice 27,6 Oxyde de fer rouge 8 Oxyde de cobalt 1 Dioxyde de manganèse 3 Notes : From Julia Moore |  | 108 - Vivian's Red/Purple/Green Aspect : Cône : 6 Composants : En masse : Néphéline syénite 46,33 Silice 19,80 Gerstley Borate 15,56 Carbonate de calcium 8,21 Dolomie 5,94 Oxyde de zinc 3,68 EPK (kaolin) 2,48 Carbonate de cuivre 0,98 Dioxyde d'étain 0,98 Rutile (Dioxyde de titane : TiO2) 0,49 Notes : In oxidation at C6, It is a transparent green that crackles. In reduction, at C6, it will turn blood red if heavily reduced,( has a tendency to run). In reduction, it works best at C10, a beautiful purple. |
| --- | --- | --- | --- | --- |

Frittes utilisées dans les recettes de ces pages :

(Formules de seger)

Fritte Pemco P-25 : K2O 0,184 Na2O 0,760 CaO 0,029 ZnO 0,028 Al2O3 0,381 B2O3 0,774 SiO2 2,629

Fritte Pemco P-311 : K2O 0,020 Na2O 0,288 CaO 0,691 Al2O3 0,270 B2O3 0,570 SiO2 2,486

Fritte Pemco P-626 : BaO 0.664 Na2O 0.336 Al2O3 0.197 B2O3 .662 SiO2 3.044

Fritte Ferro 3110 : K2O 0,064 Na2O 0,644 CaO 0,293 Al2O3 0,095 B2O3 0,097 SiO2 3,003

Fritte Ferro 3124 : K2O 0,020 Na2O 0,282 CaO 0,698 Al2O3 0,269 B2O3 0,547 SiO2 2,555

Fritte Ferro 3134 : Na2O 0,317 CaO 0,683 B2O3 0,634 SiO2 1,476

Fritte Ferro 3191 : Na2O 0,501 CaO 0,499 B2O3 1,002 SiO2 2,000

Fritte Ferro 3195 : Na2O 0,313 CaO 0,686 Al2O3 0,404 B2O3 1,099 SiO2 2,751

Fritte Ferro 3230 : BaO 0,03 K2O 0,25 Na2O 0,64 ZnO 0,08 SiO2 2,26

Fritte Ferro 3278 : Na2O 0,669 CaO 0,331 B2O3 0,842 SiO2 2,530

Fritte Ferro 3289 : Na2O 0.332 BaO 0.668 Al2O3 0.198 B2O3 0.668 SiO2 3.070

Fritte Ferro 3304 : Na2O 0,07 PbO 0,93 Al2O3 0,15 SiO2 2,58

Fritte Ferro 3403 : Na2O 0.015 K2O 0.046 CaO 0.005 PbO 0.934 Al2O3 0.069 SiO2 1.438

Matières typiques Nord Américaines :

(Les compositions sont données en % massiques)

Ocmulgee red clay : A sandy, coarse, iron-bearing clay formed by sedimentary deposition by moving water. Composition % 0.358 Na2O 1.285 K2O 0.793 MgO 0.37 CaO 21.82 Al2O3 53.86 SiO2 1.196 TiO2 6.4 Fe2O3 0.230 MnO 8.9 Perte au feu

Pine lake fire clay : Composition % 0.2 Na2O 0.6 K2O 0.1 MgO 0.3 CaO 27.3 Al2O3 58.6 SiO2 1.9 TiO2 1.5 Fe2O3 9.5 Perte au feu

Goldart stoneware : A plastic Ohio fire clay / stoneware clay. Formed by metamorphosis of an ancient swamp. Composition % 0.17 Na2O 1.00 K2O 0.23 MgO 0.09 CaO 28.53 Al2O3 57.46 SiO2 1.99 TiO2 1.25 Fe2O3 9.28 Perte au feu.

Kentuky OM#4 ball clay : OM #4 is a fine-grained ball clay with good plasticity and strength. It is very common in glaze recipes. It undergoes a sudden color shift around cone 8-9, from straw yellow to solid gray [IMC]. Composition % 0.3 Na2O 1.0 K2O 0.4 MgO 0.3 CaO 27.9 Al2O3 55.2 SiO2 1.2 TiO2 1.1 Fe2O3 12.6 Perte au feu.

Barnard clay : A high-iron clay from glacial deposits. Composition % 0.12 Na2O 2.04 K2O 0.75 MgO 0.27 CaO 10.87 Al2O3 59.7 SiO2 0.67 TiO2 14.65 Fe2O3 3.4 MnO 7.48 Perte au feu.

Grolleg china clay (exception cette matière est Anglaise): A primary (residual) kaolin formed by the action of hydrothermal vapors on soda feldspar in granites and pegmatites. 81% kaolinite, 15% mica, 4% feldspar and other minerals. Manufactured by ECC International; comes from southwest England. Plastic and white-firing, low shrinkage, excellent hardness. Composition % 0.10 Na2O 1.90 K2O 0.10 CaO 0.30 MgO 37.00 Al2O3 48.00 SiO2 0.03 TiO2 0.70 Fe2O3 12.01 Perte au feu

A.P green fire clay : A Missouri fire clay - a secondary deposit of clay and sediment in deep fresh water. Composition % 1.0 K2O 0.35 MgO 0.35 CaO 31.0 Al2O3 52.0 SiO2 1.9 TiO2 2.0 Fe2O3 11.0 Perte au feu.

Tennessee #9 Ball Clay : Off-white, light-firing ball clay. Contains 74% kaolinite, 17% free quartz, 5% feldspar, and 1% organic material. Composition % 0.3 Na2O 0.4 K2O 0.4 MgO 0.5 CaO 30.1 Al2O3 54.2 SiO2 1.6 TiO2 1.1 Fe2O3 11.4 Perte au feu.

Kingsley Kaolin : A coarse white-firing kaolin. Composition % 0.11 Na2O 0.14 K2O 0.04 MgO 0.90 CaO 38.40 Al2O3 44.80 SiO2 1.64 TiO2 0.39 Fe2O3 13.60 Perte au feu.

P.B.X fire clay : A Missouri fire clay. Missouri fire clays are secondary deposits of clay and sediment formed in deep fresh waters. Composition % 0.35 MgO 0.36 CaO 38.52 Al2O3 56.63 SiO2 1.51 TiO2 1.75 Fe2O3 0.88 Perte au feu.

Kona F4 Feldspar : Commonly used soda feldspar; used in porcelains because of its low iron content. Composition % 6.90 Na2O 4.8 K2O 0.05 MgO 1.70 CaO 19.60 Al2O3 66.80 SiO2 0.04 Fe2O3 0.20 Perte au feu.

Albany slip : An iron-rich clay consisting of shale, slate, limestone, sandstone, and dolomite deposits from glacial Lake Albany during the Wisconsin Ice Age (10-15 thousand years ago). Contains illite, quartz, limonite, chlorite, calcite, dolomite, and kaolinite. Composition % 0.80 Na2O 3.20 K2O 2.71 MgO 5.81 CaO 14.63 Al2O3 57.82 SiO2 0.40 TiO2 5.21 Fe2O3 9.41 Perte au feu.

G200 Feldspar : Commonly used potash feldspar. In many cases can be substituted for or by Custer. Composition % 3.04 Na2O 10.75 K2O 0.81 CaO 18.5 Al2O3 66.3 SiO2 0.082 Fe2O3 0.16 Perte au feu.

Custer Feldspar : Commonly used potash feldspar. Can be used to substitute for Keystone, Buckingham, Yankee, or Kingman feldspars. Composition % 2.91 Na2O 10.28 K2O 0.30 CaO 17.35 Al2O3 69.00 SiO2 0.12 Fe2O3 0.04 Perte au feu

Volcanic ash : Aluminosilicate glass of volcanic origin. Results when a volcano blows tiny particles of frothy lava into the air; these particles settle for many miles around, sometimes in layers over 30 feet deep. Variable in composition. Composition % 1.79 Na2O 7.84 K2O 0.07 MgO 0.68 CaO 11.55 Al2O3 72.51 SiO2 0.10 P2O5 0.54 TiO2 1.20 Fe2O3.

Epsom salts : magnesium sulfate. Highly soluble; used in small quantities (0.1%-1%) as a flocculant in slips and glazes. Many sources recommend making a concentrated solution, then adding the solution to the mixed glaze. Composition Molaire : MgO SO3 7 H2O.

Alberta Slip : substitute for Albany slip. Composition % 2.00 Na2O 3.35 K2O 3.32 MgO 6.30 CaO 0.19 BaO 14.56 Al2O3 64.83 SiO2 0.46 TiO2 5.01 Fe2O3

K200 Feldspar : Potash feldspar. Composition % 3.36 Na2O 10.13 K2O 0.18 CaO 17.84 Al2O3 67.99 SiO2 0.08 Fe2O3 0.31 perte au feu.

Red Art : An iron-rich clay consisting of clay/shale deposits from a prehistoric lake bed. Contains 40% illite, 10% kaolinite, 7% iron oxide, and 15% mixed layered clays. Composition % 0.38 Na2O 4.15 K2O 1.59 MgO 0.26 CaO 15.51 Al2O3 64.95 SiO2 1.09 TiO2 7.05 Fe2O3 0.22 P2O5 4.80 Perte au feu.

Cryolite : A natural source of insoluble sodium. Because of its lack of oxygen, can help to produce artifical reduction in electric firing. The release of fluorine at higher temperatures may produce cratered, bubbled surfaces. Composition : Na3AlF6

Opax : Fritted zirconium opacifier. No longer manufactured. Composition % 1.11 Na2O 0.91 Al2O3 6.48 SiO2 90.84 ZrO2

Cornwall stone : Composition % 3.30 Na2O 4.31 K2O 0.14 MgO 1.81 CaO 16.31 Al2O3 73.80 SiO2 0.15 TiO2 0.20 Fe2O3